## Slide 1
IEEE TRANSACTIONS ON NANOTECHNOLOGY · MANUSCRIPT IN PREPARATION
Device-Guided Calibration of the
Stanford RRAM Compact Model
Generalization, Identifiability, and Deposition Trends in
Sputter-Deposited TaOₓ Devices
Md Tawsif Rahman Chowdhury · Alireza Moazzeni · Gozde Tutuncuoglu
Department of Electrical & Computer Engineering, Wayne State University
Fit quality is not enough — we also report cycle-to-cycle generalization and parameter identifiability with every extraction.

## Slide 2
MOTIVATION
A good overlay is necessary — but not sufficient
▸ Compact models are usually calibrated by matching one measured I–V loop. A clean overlay can be reached even when very different parameter sets fit equally well.
▸ The risk: fit knobs get mistaken for material/process information — two fits with identical butterfly curves can disagree on Eₐ, Rₛ, or gap geometry.
▸ We separate two questions rarely reported for RRAM:
Generalization
Does a fit to one representative cycle predict the other measured cycles of the same device?
Identifiability
Which fitted parameters stay stable when the measured cycle population is resampled?
Our position
Reliable compact-model extraction must report three things together:
1 Fit quality
2 Cycle-to-cycle generalization
3 Parameter identifiability
…plus conduction-regime validity, so we know where the device physics sits outside the model.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
2

## Slide 3
DEVICES & EXPERIMENT
Twelve TaOₓ deposition conditions (DOE)
▸ Sputter-deposited TaOₓ cross-point RRAM, 4 µm feature, asymmetric Ta-oxide bilayer stack.
▸ Two fab-facing knobs: O₂ fraction (20–35%) and RF sputter power (75–250 W).
▸ Face-centered factorial with 4 replicated center points (S9–S12) — lets us test which extracted parameter is stable enough to plot vs. process.
▸ Bipolar DC switching on a Keysight B1500; automated quality screen rejects shorted / open / noise-floor sweeps.
▸ S1 reference device: all 40 cycles pass, mean quality 8.9/10.
Sample | O₂ (%) | Power (W)
S1 | 20 | 75
S2 | 20 | 250
S3 | 35 | 75
S4 | 35 | 250
S5 | 20 | 162.5
S6 | 35 | 162.5
S7 | 27.5 | 75
S8 | 27.5 | 250
S9–S12 | 27.5 | 162.5 (×4 center)
Deposition design of experiments (Table I).
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
3

## Slide 4
METHODOLOGY
A device-first extraction pipeline
1
Medoid cycle
pick the representative measured sweep by ranked quality
2
Regime classify
ohmic / PF / Schottky / FN per segment
3
Physics priors
regime-tied prior windows for 21 parameters
4
Mechanism loss
down-weight Schottky/FN points the model can't represent
5
Bayesian opt.
HSPICE-in-the-loop, 48+160 evals, then Nelder–Mead
6
Generalization
score the medoid fit on every other cycle
7
Identifiability
200 cycle-bootstrap refits + Fisher cross-check
8
Ablation
isolate what priors / regime / BO each contribute
Stanford–PKU Verilog-A model (rram_v_1_0_0): Iₜₕ = I₀·exp(−g/g₀)·sinh(V/V₀), gap evolves thermally. Polarity-split V₀, Eₐ, ν₀, g; shared scale/parasitic terms. 616 HSPICE transients per point estimate.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
4

## Slide 5
RESULT 1 · DEVICE PHYSICS
Ohmic LRS, Schottky-limited HRS — across the whole DOE
S1 regime classification of the four resistance-state segments (Fig. 1).
Dominant mechanism & cycle stability, all 12 conditions (Fig. 2).
▸ Post-SET LRS is ohmic-dominant for every condition (66–100% stability).
▸ Post-RESET HRS is Schottky-dominant in 92.5–100% of cycles, εᵣᵈʸⁿ = 4.7–34 (physically admissible).
▸ PF is rare — it is not the dominant mechanism for any state/condition.
▸ Implication: Stanford bulk sinh law has no explicit Schottky branch → expect a RESET residual floor.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
5

## Slide 6
RESULT 2 · POINT ESTIMATE
The fits reproduce the measured butterfly curves
0.530
Mean SET RMSE
log₁₀|I| decades
0.761
Mean RESET RMSE
harder: Schottky HRS
Cond. | RMSE SET | RMSE RESET | DW SET | DW RESET
S1 | 0.500 | 0.689 | 0.86 | 0.85
S2 | 0.772 | 1.016 | 0.46 | 0.56
S6 | 0.468 | 0.650 | 0.94 | 0.93
S8 | 0.495 | 1.001 | 1.03 | 0.54
Mean | 0.530 | 0.761 | — | —
Excerpt of Table II (12 conditions total).
▸ Captured: hysteresis order, SET & RESET transitions, compliance region, LRS return branch.
▸ Largest residuals sit at the SET transition and the Schottky-limited HRS approach — exactly where the regime map warned the current law is incomplete.
▸ Durbin–Watson < 2 everywhere: residuals are correlated along the sweep — remaining error is systematic model mismatch, not measurement scatter.
▸ S2 is the worst case (O₂-poor, high power): largest RESET RMSE, lowest SET DW, least stable Schottky assignment.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
6

## Slide 7
RESULT 3 · GENERALIZATION
A one-cycle fit predicts every other cycle
Held-out per-cycle RMSE; stars = in-sample medoid (Fig. 4).
S1 fit vs. measured cycle-to-cycle envelope (Fig. 5).
0.012
SET gap
held-out − in-sample
0.039
RESET gap
decades
▸ Held-out medians 0.542 (SET) / 0.800 (RESET) vs. in-sample 0.530 / 0.761.
▸ Every condition: in-sample RMSE falls inside the held-out interquartile range.
▸ Coverage: fitted SET curve stays inside the measured min–max band at 77% of points (63% for RESET).
▸ Takeaway: the fit describes the device population — not a memorized trace. Lower RESET coverage = missing Schottky branch, not overfitting.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
7

## Slide 8
RESULT 4 · IDENTIFIABILITY
What the DC data actually constrain
Cycle-bootstrap CV, 200 refits × 12 conditions — primary evidence (Fig. 6).
▸ Repeatable: branch voltage scales V₀, median CV ≈ 0.28 — the butterfly curvature pins them down.
▸ Not repeatable: Rₛ (CV 1.44), velocity prefactors ν₀ (1.19 / 1.28), I₀ and Eₐ also vary widely (CV > 1).
▸ Fisher cross-check agrees on the broad picture, but condition numbers 10¹⁸–10⁶⁶ make it a local sensitivity map only.
▸ Rₛ is the cautionary case: looks locally well-determined at one optimum, yet swings under cycle resampling.
Bottom line
DC butterfly data constrain effective branch scales & switching-field combinations — not a unique split into prefactors, activation energies, and gap geometry.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
8

## Slide 9
RESULT 5 · ABLATION
What each ingredient actually buys
Variant | RMSE SET | RMSE RESET
Regime-conditioned + weighting | 0.530 ± 0.081 | 0.761 ± 0.123
Physics priors + BO | 0.546 ± 0.077 | 0.756 ± 0.124
Uninformative priors + BO | 0.537 ± 0.076 | 0.755 ± 0.126
Physics priors, no BO | 0.571 ± 0.115 | 1.528 ± 0.434
Unweighted validation RMSE so weighting gives no scoring advantage (Table IV).
▸ Optimization is the must-have: no-BO RESET balloons to 1.53 decades vs. ~0.76 for optimized variants.
▸ Three optimized variants land at nearly identical overlay error.
▸ So priors/regime don't lower the overlay — they stop the fit from abusing unsupported Schottky/FN HRS regions to distort Stanford bulk parameters.
▸ Reinforces the thesis: overlay alone can't establish physical extraction. Generalization + identifiability decide what's trustworthy.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
9

## Slide 10
RESULT 6 · PROCESS TRENDS
Only identifiable parameters get a response surface
Bootstrap-identifiable parameters vs. deposition (Fig. 8).
Post-RESET HRS dynamic permittivity vs. O₂ and power (Fig. 9).
▸ V₀,SET and V₀,RESET have tight bootstrap CIs and move systematically with deposition → usable process trends.
▸ Rₛ spans 1–2 decades in its bootstrap CI — locally Fisher-identifiable, but must NOT be a response-surface output.
▸ HRS εᵣᵈʸⁿ = 4.7–32 for all 12 conditions; ~3× scatter across center points (S9–S12) reveals interface variability — an automated extension of prior manual analysis.
Device-Guided Calibration of the Stanford RRAM Model · Chowdhury, Moazzeni, Tutuncuoglu · Wayne State University
10

## Slide 11
TAKEAWAYS
Report extraction with three numbers, not one
Fits are accurate — Mean RMSE 0.530 (SET) / 0.761 (RESET) decades across all 12 TaOₓ conditions.
…and they generalize — One-cycle fit predicts held-out cycles within 0.012 / 0.039 decades — the device, not one trace.
Most parameters aren't identifiable — Only branch voltage scales V₀ are repeatable (CV ≈ 0.28); Rₛ, ν₀, Eₐ, gap geometry are not (CV > 1).
Process trends, conservatively — Only V₀ supports a deposition response surface; Rₛ cannot, despite looking locally identifiable.
Model adequacy is the RESET floor — Post-RESET HRS is Schottky-dominant in 92.5–100% of cycles — outside the Stanford bulk sinh law.
Next: add a barrier-limited HRS branch to the compact model — the regime map already supplies the target windows and slopes.